3990 Shieldoseal导电元件粘合剂

Conductive 1-component adhesive导电元件粘合剂

Shieldoseal creates a electricaly and thermally conductive connection between components. One of the applications is EMI shielding. Shieldoseal has excellent filling properties, therefore uneven surfaces can be filled.

Shieldoseal导电元件粘合剂在元件之间建立了一个电的和热的导电连接。应用之一是EMI屏蔽。Shieldoseal导电元件粘合剂有卓越的填充特性，因此粗糙表面能被填充。

Shieldoseal cures quickly at room temperature. When fully cured, they remain as elastic as rubber and are homogenous conductive. In addition, they distinguish themselves by an especially high level of heat conductivity.

Shieldoseal在室温中快速凝固。当完全凝固时，他们仍然像橡胶一样有弹性，是同质导电的。另外，它们辨别自身通过一个特别高级的热导率。

It is pasty and can glue metals (copper, alluminium, stainless steel, brass, ect.), ceramics and most plastics. Properties for individual applications are listed in the table below.

它是面糊状的，能粘接金属（铜，铝，不锈钢，玻璃，等等），陶瓷和大多数塑料制品。独特的应用特性被列在下表中。

Specifications规格说明

|  | Unit单位 | 3390. |
| --- | --- | --- |
| Conductive particules |  | Ag/Cu |
| Desity DIN 53479 | g/cm3 | 2.4 |
| Shore A hardness DIN 53505 | +/- 6 | 62 |
| Volume resistance VDE 0303 | Ohm-cm | 0,08 |
| Temperature range | °C | -55 / +125 |
| Elolngation at break Din 53504-S1 | % | >35 |
| Color颜色 |  | Beige米色 |

Shielding performance屏蔽性能

Conductive adhesive导电粘合剂

|  | Unit单位 | 3390. |
| --- | --- | --- |
| Metal with metal |  | Good |
| Metal with RFI gasket |  | Good |
| RFI gasket with RFI gasket |  | Good |
| Adhesion on aluminium |  | > 18 |
| Viscosity upon delivery |  | Viscous |
| Tolulene solvent | N/cm | 5 |
| Catalyst | 21 °C | Air humidity |
| Resistance against | UV, ozone | Yes |
| Storage time: plastic cartridges | Weeks | 2 |
| Storage time: aluminium | Weeks | 8 |

Curing固化

|  | Unit | 3390. |
| --- | --- | --- |
| Curring at room temperature | 21 °C | Yes |
| Film formation at 0,2 mm strength approx | Minutes | 1 - 4 |
| Curing at 0,2 mm strength approx | Minutes | 5 - 20 |
| Curing based on film strength and venting surface approx. | Minutes | 3 - 180 |
| Odorless |  | No |

Example举例

When you want to order 3990 Shieldoseal please specify the following:

| Partnumber | Content (ml) | Quantity |
| --- | --- | --- |
| 3990 | 10 | 1 |
|  | 10 ml - plastic cartridge Standard package of 10 ml, other on request |  |