5711 - 5722 Oriented wire shield定向的导线屏蔽

| Sheet material to die-cut complicated shapes薄板材料冲切为复杂形状 Oriented Wire Shield 5711 - 5722 is a composite gasket material consisting of a large number of small wires embedded and bonded in solid or sponge silicone, or fluor silicone elastomer for oil-resistance. The wires provide excellent conductivity to establish EMI / RFI shielding. 定向导线屏蔽5711-5722是一个合成的垫片材料，由大量的小导线嵌入和被接合在固体或海绵硅树脂里，或氟硅树脂人造橡胶用于耐油性。 导线提供良好的导电性以建立EMI/RFI屏蔽。 The Material is used in military, industrial and commercial products requiring EMI suppression, grounding, or static discharge. It is very suitable for applications where an environmental or pressure seal is required. 该材料被使用在军事，工业和商业产品要求EMI抑制，接地，或静电放电。它是非常适合于应用在一个要求环境或压力封闭。 The sponge version is used in cases of severe joint unevenness, or if lower closure forces or greater compressibility are required. 该海绵形式被使用在严重的接合不平坦的情形，或如果更低的闭合力或更大的压缩率是需要的。 |  |
| --- | --- |

Dimensions尺寸

Standard sheet of 90 x 900 mm. Bigger items can be welded/joint together. This is to prevent waste of material.

标准的薄板是90 x 900mm。大的项目能被焊接/接合在一起。这是为了预防材料的浪费。

Custom compositions are available on request, please send a drawing with dimensions to our email address

| Technical specifications技术规格 | Part numbers零件号 |
| --- | --- |
| Colour颜色: Grey silicone灰色硅树脂 Elastomer人造橡胶: Silicone or fluorosilicone Conductive filler导电填充料: Monel wire, aluminium wire ROHS compliance: Yes Corrosion resistance耐蚀性: Yes UV resistamce耐紫外线: Yes Oil resistance耐油性: Fluerosilicone type only Fuel resistance耐燃烧性: Fluorosilicone type only IP rating: Yes | Material材料 Part number Solid silicone with monel wire 5711 Solid silicone with aluminium wire 5712 Solid fluorsilicone with monel wire 5713 Sponge silicone with monel wire 5721 Sponge silicone with aluminium wire 5722 |

Available thicknesses可用的厚度

0.81, 1.13, 1.38, 1.57, 2.40, 3.18, 3.96, 4.78, 6.35 mm.

Other thicknesses on request.其它的厚度根据需求。

Performance性能

| Material材料 | Solid silicone with monel wire固体硅树脂用蒙乃尔电线 5711 | Solid silicone with aluminium wire固体硅树脂用铝线 5712 | Solid fluorosilicone with monel wire固体氟硅树脂用蒙乃尔电线 5713 | Sponge silicone with monel wire海绵硅树脂用蒙乃尔电线 5721 | Sponge silicone with aluminium wire海绵硅树脂用铝线 5722 |
| --- | --- | --- | --- | --- | --- |
| Color颜色 | Grey灰 | Grey灰 | Blue蓝 | Grey灰 | Grey灰 |
| Wire count/ sq.inch. | 900 | 900 | 900 | 900 | 900 |
| Compression set | 25% | 25% | 25% | 25% | 25% |
| Closing force 闭合力(psi) | 25-100 | 25-100 | 25-100 | 5-50 | 5-50 |
| Fuel/Solvent resistant | No | No | Yes | No | No |
| Shielding (db)屏蔽: |
| 200 KHz | 70 | 70 | 70 | 70 | 70 |
| 100 MHz | 125 | 100 | 100 | 120 | 85 |
| 1.0 GHz | 125 | 100 | 100 | 125 | 70 |
| Temperature (Cº) | -65/200 | -65/200 | -55/200 | -65/200 | -65/200 |

Benefits好处

- Temperatures up to 220°C; 温度可达220°C;

- High shielding performance; 高屏蔽性能；

- Water sealing, up to 10 meter; 水封，可达10米；

- Pressure resistant; 耐压；

- Salt spray / chemical resistant; 耐盐沫/化学品；

- Fluor-silicone rubber for fuel/oil-resistance; 氟-硅树脂橡胶用于耐燃料/石油；

- Supplied as sheets, strips or die-cuts;可供应为薄板，带或冲切；

Example举例

When ordering Flatshield 5700 please specify part number and dimensions. For die cuts, please enclose a detailed drawing.

当订购Flatshield 5700时请指定零件号和尺寸。对于冲切，请附上一个零件图。

| Series系列 | Width(mm)宽度 | Length(mm)长度 | Thickness厚度 |
| --- | --- | --- | --- |
| 5711 | 50 | 50 | 081 |
| 5711 : Solid silicone with Monel wires固体硅树脂带蒙乃尔铜-镍导线 5712 : Solid silicone with aluminium wires固体硅树脂带铝线 5713 : Solid fluorsilicone with Monel wires固体氟硅树脂带蒙乃尔铜镍导线 5721 : Sponge silicone with Monel wires海绵硅树脂带蒙乃尔铜镍导线 5722 : Sponge silicone with aluminium wires海绵硅树脂带铝线 |  |  | Available thicknesses厚度 0.81, 1.13, 1.38, 1.57, 2.40, 3.18, 3.96, 4.78, 6.35 mm. Other thicknesses on request. 其它的厚度根据需求。 |